SECTION 084113 - ALUMINUM STOREFRONT

GENERAL

RELATED DOCUMENTS

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

SUMMARY

This Section includes pre-engineered, thermally broken center glazed aluminum screw spline storefront and related accessories.

Related Sections include the following:

Division 08 Section "Glazed Aluminum Curtain Wall" for coordination among aluminum fenestration units.

Division 08 Section "Glazing" for additional glazing requirements.

Division 08 Section "Aluminum Windows" for incorporating aluminum windows into glazed curtain walls and for coordination among aluminum fenestration units.

REFERENCES

AAMA – Aluminum Storefront and Entrance manual 1989.

ASTM E283 – Standard test method for determining the rate of air infiltration through exterior framing systems under specified pressure differences across the specimen; 1991 (Reapproved 1999).

ASTM E331 – Standard test method for water penetration of exterior windows, skylights, doors and curtain walls by uniform static air pressure difference; 2000.

ASTM E330 – Standard test method for structural performance of exterior windows, doors, skylights and curtain walls by uniform static air pressure difference; 2001.

AAMA 1503/1/98 – Test method for condensation resistance factor (CRF) and test method for thermal transmission coefficient (U Value).

AAMA 501.2 – Field check of metal storefronts, curtain walls, and sloped glazing systems for water leakage; 1994 (part of AAMA 501).

PERFORMANCE REQUIREMENTS

Structural Performance:  Provide aluminum storefront capable of withstanding the effects of the following loads as well as the design wind load indicated but in no case less than 30 psf.

Uniform Load Deflection Test:  No deflection of any unsupported span L of test unit in excess of L/175 at a test pressure of 60 psf (positive and negative) when test in accordance with ASTM E330.

Uniform Load Structural Test:  Units to be tested at 90 psf or 1.5 times the design pressure (positive and negative) acting normal to the plane of the wall in accordance with ASTM E330.

No glass breakage or permanent set of any main frame member in excess of 0.2% of its clear span.

SUBMITTALS

Product Data:  Include construction details, material descriptions, fabrication methods, dimensions of individual components, profiles, and finishes.

Shop Drawings:  Include plans, elevations, sections, details, attachments to other work, installation details, and the following:

Mullion details, including reinforcement and stiffeners.

Joinery details.

Weather-stripping details.

Glazing details.

Samples for Initial Selection:  For units with factory-applied color finishes.

Maintenance Data:  Include cleaning instructions for glass and metal finishes in maintenance manuals.

Test Reports and Calculations:

Submit certified independent laboratory test reports showing compliance with the specified requirements.

[Submit structural calculations prepared by a registered New Jersey Professional Engineer showing compliance with the specified uniform and structural load requirements.]

QUALITY ASSURANCE

Engineering Responsibility:  Shop drawings and engineering analysis shall be performed by aluminum storefront manufacturer.

Product Requirements:  For maximum performance, the storefront for this project must meet both the testing requirements as contained herein and the minimum material requirements specified.

Installer Qualifications:  An installer acceptable to aluminum storefront manufacturer for installation of units required for this Project.

Source Limitations:  Obtain aluminum storefront, curtain wall and windows through one source from a single manufacturer.

Product Options:  Drawings indicate size, profiles, and dimensional requirements of aluminum storefront and are based on the specific system indicated.  Do not modify size and dimensional requirements.

Do not modify intended aesthetic effects, as judged solely by Architect, except with Architect's approval.  If modifications are proposed, submit comprehensive explanatory data to Architect for review.

Glazing Publications:  Comply with published recommendations of glass manufacturers and with GANA's "Glazing Manual" unless more stringent requirements are indicated.

Preinstallation Conference:  If requested, conduct conference at project site to review methods and procedures related to aluminum curtain wall including, but not limited to, the following:

Review and finalize construction schedule and verify availability of materials, Installer's personnel, equipment, and facilities needed to make progress and avoid delays.

Review, discuss, and coordinate the interrelationship of aluminum curtain wall with other exterior wall components.

Review and discuss the sequence of work required to construct a watertight and weathertight exterior building envelope.

Inspect and discuss the condition of substrate and other preparatory work performed by other trades.

PROJECT CONDITIONS

Field Measurements:  For retrofit installations, verify aluminum storefront openings by field measurements before fabrication and indicate measurements on Shop Drawings.

Established Dimensions:  Where field measurements cannot be made without delaying the Work, establish opening dimensions and proceed with fabricating aluminum curtain wall without field measurements.  Coordinate wall construction to ensure that actual opening dimensions correspond to established dimensions.

WARRANTY

Special Warranty:  Manufacturer's standard form in which manufacturer agrees to repair or replace aluminum storefronts that fail in materials or workmanship within specified warranty period.

Failures include, but are not limited to, the following:

Failure to meet performance requirements.

Structural failures including excessive deflection, water leakage, or air infiltration.

Deterioration of metals or other materials beyond that which is normal.

Failure of insulating glass.

Warranty Period:

Storefront: [Two] [Three] [Five] [Ten] years from date of Substantial Completion.

[Insulated Glazing:  10 years from date of Substantial Completion.]

[Painted Metal Finishes:]

[Five years from date of Substantial Completion for AAMA 2603 Baked Enamel Finishes.]

[Ten years from date of Substantial Completion for AAMA 2604 High Performance Finishes.]

[Twenty years from date of Substantial Completion for AAMA 2605 Superior Performance Finishes.]

PRODUCTS

MANUFACTURERS

Basis-of-Design Product:  The basis of design for these specifications is the Series 1700 Aluminum Storefront as manufactured by Architectural Window Manufacturing Corporation, Rutherford, New Jersey.

Equivalents:  Subject to compliance with all material and performance requirements outlined in these specifications, “or equal” products by other manufacturers will be considered for use subject to review by the Architect.  The Architect’s decision regarding equivalency is final.

MATERIALS

Aluminum Extrusions:  Extruded aluminum prime billet 6063-T5 recommended by aluminum curtain wall manufacturer for strength, and application of required finish to meet the requirements of ASTM B221 and not less than 0.080-inch thickness at any location.

Face Dimension/Frame Depth:  2” face dimension; 4 ½” frame depth.

Fasteners:  Aluminum, nonmagnetic stainless steel, epoxy adhesive, or other materials warranted by manufacturer to be noncorrosive and compatible with aluminum storefront members, anchors, and other components.

All fasteners must be concealed except where unavoidable for application of hardware.

For application of hardware, where required, use non-magnetic stainless steel phillips machine screws.

Anchors, Clips, and Accessories:  Aluminum, nonmagnetic stainless steel, or zinc-coated steel or iron complying with ASTM B 633 for SC 3 severe service conditions; provide sufficient strength to withstand design pressure indicated.

Framing Gaskets:  Comply with ASTM C864-99, Option II; EPDM, in a hardness suitable for its intended use.  70 Shore A Durometer for Preset Gaskets.  Black.  All corners of glazing gaskets shall be bed in silicone sealant compatible with glazing gaskets.

Setting Blocks:  EPDM85 Shore A Durometer; minimum 4” long per glass manufacturer’s requirements.

Sealant:  For sealants required for assembly of aluminum storefront, provide manufacturer's standard, permanently elastic, nonshrinking, and nonmigrating type recommended by sealant manufacturer for joint size and movement.

STOREFRONT

Storefront Type:  Screw spline

Condensation-Resistance Factor (CRF):  Provide aluminum storefront tested for thermal performance according to AAMA 1503, showing a minimum CRF of 60.

Provide aluminum storefront with a U-factor and SHGC maximums indicated when simulated in accordance with NFRC 100 and NFRC 200 at the two-lite model size of 79” x 79” and glazed with 1” Argon filled sputter coat Low-E (#3) insulated glass using a warm edge spacer.

U-Factor:  0.36 Btu/sq. ft. x h x deg F or less.

SHGC:  0.34.

Air Infiltration:  Maximum rate not more than indicated when tested according to ASTM E283, Air Infiltration Test.

Maximum Rate:  <0.01 cfm/sq. ft. of area at an inward test pressure of 6.24 lbf/sq. ft. (300 Pa).

Water Resistance:  No uncontrolled water leakage at a static water test pressure equaling that indicated, when tested according to ASTM E331, Water Resistance Tests.

Test Pressure:  30 lbf/sq. ft.

INSULATED GLAZING

Construction:  All storefront (except those receiving insulated panels) shall be field glazed with hermetically sealed 1” insulating glass units with a dual seal of polyisobutylene and silicone and a desiccant filled spacer.  Insulated glass shall be dry glazed and held in place with recyclable EPDM gaskets on both the exterior and interior and must be glazed in accordance with GANA Glazing Manual for the specified glass type.

Exterior Glazing:

Thickness: [1/8”] [3/16”] [1/4”] [5/16”]

Tint: [Clear] [Bronze] [Grey] [Green]

Type: [Annealed Glass] [Heat Strengthened Glass] [Tempered Glass] [Laminated Glass (.030” PVB Interlayer)] [Laminated Glass (.060” PVB Interlayer)] [Laminated Glass (.090” PVB Interlayer)]

[Coating: [Pyrolitic Low-E (#2 Surface)] [Guardian SuperNeutral 68, Vitro Solarban 60, Viracon VE-2M Low-E (or equal) (#2 Surface)] [Other (Insert requirements or contact AWM for assistance)]]

Interior Glazing:

Thickness: [1/8”] [3/16”] [1/4”] [5/16”]

Tint: [Clear] [Obscure]

Type: [Annealed Glass] [Heat Strengthened Glass] [Tempered Glass] [Laminated Glass (.030” PVB Interlayer)] [Laminated Glass (.060” PVB Interlayer)] [Laminated Glass (.090” PVB Interlayer)]

[Coating: [Pyrolitic Low-E (#3 Surface)] [Guardian SuperNeutral 68, Vitro Solarban 60, Viracon VE-2M Low-E (or equal) (#3 Surface)] [Other (Insert requirements or contact AWM for assistance)]]

Interspace Content: [Air] [Argon]

Spacer Type: [Aluminum] [Warm Edge]

Opaque Insulated Panels:

Overall thickness: [1/4”] [1”]

Exterior Face: [Kynar paint on [smooth] [textured] .032” aluminum] [Porcelain enamel on 28 gauge [smooth] [textured] steel] - color to be selected from manufacturer’s standard.

Interior Face: [Kynar paint on [smooth] [textured] .032” aluminum] [Porcelain enamel on 28 gauge [smooth] [textured] steel] - color to be selected from manufacturer’s standard.

Exterior Substrate: [1/8” hardboard.] [3/16” mineral fiber board.] [3/16” corrugated plastic.]

Interior Substrate: [1/8” hardboard.] [3/16” mineral fiber board.] [3/16” corrugated plastic.] [1/2” Type C Firecode gypsum board.]

Core: [Polyisocyanurate.] [Polystyrene.]

HARDWARE

General:  Not applicable (See Division 8 Section “Aluminum Windows” for operable window requirements.)

INSECT SCREENS

General:  Not applicable (See Division 8 Section “Aluminum Windows” for operable window requirements.)

ACCESSORIES

Rescue Labels:  Not applicable.

FABRICATION

Shop fabricate screw-spline aluminum storefront per manufacturer’s instructions.  Include a complete system for assembling components and anchoring storefronts.

Thermally Improved Construction:  Aluminum storefront framing shall be thermally broken using a concealed, chemically curing two-part high-density polyurethane pour and debridged type structural thermal barrier.  A non-structural thermal barrier is not acceptable.

Weather Stripping:  Weather stripping shall be closed cell EPDM installed in integral raceways in framing members and pressure plates.

Weep Holes:  Provide weep holes and internal passages to conduct infiltrating water to exterior.

Muntins:  Where shown on drawings, muntins shall be roll formed aluminum between the lites of 1” deep insulated glass.

FINISHES, GENERAL

Comply with NAAMM's "Metal Finishes Manual for Architectural and Metal Products" for recommendations for applying and designating finishes.

Finish designations prefixed by AA comply with the system established by the Aluminum Association for designating aluminum finishes.

Exterior & Interior of Storefront:

[Class II, Clear Anodic Finish:  AA-M12C22A31 (Mechanical Finish:  nonspecular as fabricated; Chemical Finish:  etched, medium matte; Anodic Coating:  Architectural Class II, clear coating 0.010 mm or thicker) complying with AAMA 611.]

[Class I, Clear Anodic Finish:  AA-M12C22A41 (Mechanical Finish:  nonspecular as fabricated; Chemical Finish:  etched, medium matte; Anodic Coating:  Architectural Class I, clear coating 0.018 mm or thicker) complying with AAMA 611.]

[Class I, Color Anodic Finish:  AA-M12C22A42/A44 (Mechanical Finish:  nonspecular as fabricated; Chemical Finish:  etched, medium matte; Anodic Coating:  Architectural Class I, integrally colored or electrolytically deposited color coating 0.018 mm or thicker) complying with AAMA 611.

Color: [Champagne] [Medium bronze] [Dark bronze] [Black].]

[Baked-Enamel Finish:  AA-C12C42R1x (Chemical Finish:  cleaned with inhibited chemicals; Chemical Finish:  acid-chromate-fluoride-phosphate conversion coating; Organic Coating:  as specified below).  Apply baked enamel complying with paint manufacturer's written instructions for cleaning, conversion coating, and painting.

Organic Coating:  Thermosetting, modified-acrylic enamel primer/topcoat system complying with AAMA 2603 Organic Coating:  Thermosetting, modified-acrylic enamel primer/topcoat system complying with AAMA 2603.

Color:  As selected by Architect from [manufacturer’s standard non-mica, non-exotic, non-metallic colors.] [manufacturer’s standard mica/metallic colors.]  (Note:  Exterior color may be different from interior color.)]

[High-Performance Organic Finish:  AA-C12C42R1x (Chemical Finish:  cleaned with inhibited chemicals; Chemical Finish:  acid-chromate-fluoride-phosphate conversion coating; Organic Coating:  as specified below).  Prepare, pretreat, and apply coating to exposed metal surfaces to comply with coating and resin manufacturer’s written instructions.

Fluoropolymer Two-Coat System:  Manufacturer’s standard two-coat thermocured system consisting of specially formulated inhibitive primer and fluoropolymer color topcoat containing not less than 50% polyvinylfluoride resin by weight; complying with AAMA 2604.

Color:  As selected by Architect from [manufacturer’s standard non-mica, non-exotic, non-metallic colors.] [manufacturer’s standard mica/metallic colors.]  (Note:  Exterior color may be different from interior color.)]

[Superior-Performance Organic Finish:  AA-C12C40R1x (Chemical Finish:  cleaned with inhibited chemicals; Chemical Finish:  acid-chromate-fluoride-phosphate conversion coating; Organic Coating: as specified below).  Prepare, pretreat, and apply coating to exposed metal surfaces to comply with AAMA 2605 and with coating and resin manufacturer’s written instructions.

Fluoropolymer [Two-Coat] [Three-Coat] System:  Manufacturer’s standard [two-coat] [three-coat] thermocured system consisting of specially formulated inhibitive primer [and fluoropolymer color topcoat containing not less than 70 percent polyvinylidene fluoride resin by weight; complying with AAMA 2605.] [, fluoropolymer color coat, and clear fluoropolymer top coat, with both color coat and clear topcoat containing not less than 70 percent polyvinylidene fluoride resin by weight; complying with AAMA 2605.]

Color:  As selected by Architect from [manufacturer’s standard non-mica, non-exotic, non-metallic colors.] [manufacturer’s standard mica/metallic colors.]  (Note:  Exterior color may be different from interior color.)]

EXECUTION

EXAMINATION

Examine openings, substrates, structural support, anchorage, and conditions, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance of work.  Verify rough opening dimensions and levelness of sill plate.  Examine wall flashings, vapor retarders, water and weather barriers, and other built-in components to ensure a coordinated, weathertight storefront installation.

Masonry Surfaces:  Visibly dry and free of excess mortar, sand, and other construction debris.

Wood Frame Walls:  Dry, clean, sound, well nailed, free of voids, and without offsets at joints.  Ensure that nail heads are driven flush with surfaces in opening and within 3 inches (76 mm) of opening.

Metal Surfaces:  Dry; clean; free of grease, oil, dirt, rust, corrosion, and welding slag; without sharp edges or offsets at joints.

Proceed with installation only after unsatisfactory conditions have been corrected.

INSTALLATION

Comply with Drawings, Shop Drawings, and manufacturer's written instructions for installing storefront, hardware, accessories, and other components.

Install storefront level, plumb, square, true to line, without distortion or impeding thermal movement, anchored securely in place to structural support.

Install storefront and components to drain condensation, water penetrating joints, and moisture migrating within storefront to the exterior.

Separate aluminum and other corrodible surfaces from sources of corrosion or electrolytic action at points of contact with other materials.

FIELD QUALITY CONTROL

Testing Agency: [If desired, Owner will engage] [Engage] a qualified testing agency to perform tests and inspections and prepare test reports.

Testing and inspecting agency will interpret tests and state in each report whether tested work complies with or deviates from requirements.

Revise first paragraph below if more stringent field testing is required to suit Project.  According to AAMA 502, Test Method A is the default, unless otherwise indicated.

Testing Services:  Testing and inspecting of installed storefront shall take place as follows:

Testing Methodology:  Testing of storefront for air infiltration and water resistance shall be performed according to [AAMA 501.2.] [AAMA 503.]  Field test pressures and allowable limits shall be as factored by [AAMA 501.2] [AAMA 503] from those minimums required to determine laboratory compliance.

Testing Extent: One test in a location selected by Architect and a qualified independent testing and inspecting agency.  Storefront shall be tested immediately after installation.

Test Reports:  Shall be prepared according to [AAMA 501.2] [AAMA 503].

Remediate noncomplying curtain wall and retest as specified above.

Additional testing and inspecting, at Contractor's expense, will be performed to determine compliance of remediated doors or additional work with specified requirements.

ADJUSTING, CLEANING, AND PROTECTION

Installer shall remove all labels and shipping bumpers from glass.

Manufacturer shall clean all aluminum prior to shipment.

Protection of newly installed storefront and/or final cleaning of glass and aluminum to remove any accumulations that may have occurred during the construction period is to be the responsibility of the General Contractor or Owner.

Comply with manufacturer’s written recommendations for final cleaning and maintenance.

DEMONSTRATION

Engage a factory-authorized service representative to train Owner's maintenance personnel to maintain storefront.

END OF SECTION 084113